Dear Editor of Journal of the Serbian Chemical Society,

The authors Carmen Steluta Ciobanu, Cristina Liana Popa, Daniela Predoi are hereby submitting to your journal the manuscript entitled: “Cerium doped hydroxyapatite nanoparticles synthesized by coprecipitation method”

In this paper we report a simple coprecipitation adapted method for the synthesis of stable Ce substituted to Ca hydroxyapatite nanoparticles. The structural and morphological properties of Ce doped hydroxyapatite (Ce:HAp) were characterized by X-ray diffraction (XRD), Scanning Electron Microscopy (SEM) and Energy Dispersive X-ray analysis (EDAX). The optical properties of Ce doped hydroxyapatite were also investigated using Fourier Transform Infrared (FTIR) spectroscopy, FT Raman spectroscopy and photoluminescence analysis. The results of the XRD studies revealed the progressive increase in the a- and c-axes with increasing of Ce concentrations. The nanometric dimensions of the particles were also confirmed by the SEM micrographs. In the FTIR studies of Ce:HAp powders a similar structure to hydroxyapatite was observed. IR and Raman wavenumbers and the peak strength of the bands associated to the P-O and O-H bonds decreases progressively with the increase of Ce concentration. The results obtained by FTIR and Raman spectroscopies confirmed the XRD analysis. All the emission maxima could be attributed to the 5d-4f transitions of Ce ions. The displacement of maximum emission bands with the increase of Cerium in the samples is in agreement with the results obtained by XRD studies.

We hope that our paper will comply with the criteria for publication in the “Journal of the Serbian Chemical Society”.

This cover letter acknowledges that the authors have consulted the Guide for Authors in preparing our submitted manuscript. The authors declare that they have no competing interests.

Finally, this paper is our original unpublished work and it has not been submitted to any other journal for reviews.

Best regards,

Dr. Daniela Predoi

List of suggested reviewers

Michel Lahaye

E-mail address: lahaye@icmcb-bordeaux.cnrs.fr

Ingénieur de Recherche - Université Bordeaux 1

tél. : 05-40-00-62-93

Roland Lang

Institute of Medical Microbiology, Immunology and Hygiene, Technical University Munich, Trogerstr. 30, 81675 Munich, Germany

Tel.: +4989 4140 7454;

fax: +4989 4140 4139.

E-mail address:Roland.Lang@lrz.tum.de (R. Lang).

Syu-ichi Kanno

Department of Pharmacology and Toxicology, Cancer Research Institute, Tohoku Pharmaceutical University, 4-4-1 Komatsushima,

Aoba-ku, Sendai 981-8558, Japan

Tel.: +81 22 234 4181x4112; fax: +81 22 275 2013.

E-mail address: syu-kan@tohoku-pharm.ac.jp (S. Kanno).

Ebbe Billmann Thorgersen

Institute of Immunology, Rikshospitalet University Hospital, University of Oslo, N-0027 Oslo, Norway

Tel.: +47 23073014; fax: +47 23073510

E-mail address: ebbtho@rr-research.no (E.B. Thorgersen)