Reviewer A

Thank you very much for your remarks

1. Next sentences must be deleted from the introduction:
"Our results revealed that cerium ions have been successfully incorporated
in the hydroxyappatite structure without altering its general structure.
However, XRD and SEM studies demonstrated that even small concentrations of
cerium induce a decrease of the crystallite size. The structural properties
also appear to be influenced by the slight increase of the cerium
concentration. FTIR and Raman studies revealed that the P-O bonding strength
decreases with the increase of cerium concentration. Also, it was shown that
the photoluminescent properties of the powders are influenced by the cerium
present in the samples. Lastly, the antimicrobial activity of the cerium
doped hydroxyapatite samples has been assessed against commonly found Gram
negative (E. coli 714) and Gram positive (S. aureus ATCC 6538) bacterial
strains."

In agreement with the reviewer comments, the sentences were removed.

2. The authors in the answer show that SEM images are changed, but in the
manuscript are the same SEM images, and from these SEM micrographs it is not
possible to see demonstrated particle size distribution.

In agreement with the reviewer comments, the size distribution calculated from SEM micrographs was removed and in order to confirm the particle dimensions obtained by XRD measurements, the size distribution was measured from the TEM micrographs.The added text was marked in yellow.