Uticaj nano- i mikro- aluminijum-oksidnih punioca na neka svojstva kompozita na bazi poli(metil metakrilata)

FATHIE KUNDIE1,3*, HUSNA AZHARI1** and ZAINAL AHMAD2

1Department of Mechanical & Materials Engineering, Faculty of Engineering & Built Environment, The National University of Malaysia, 43600 Bangi, Selangor, Malaysia

2School of Material and Mineral Resource Engineering, University Sains Malaysia,14300 Nibong Tebal, Pulau Pinang, Malaysia

3Department of Dental Technology, College of Medical Technology, P.O. Box 1458, Misurata, Libya

*’** Corresponding authors. E-mail: (*)fathie2@yahoo.com; (**)husna.azhari@gmail.com

Apstrakt: U okviru ovog rada su prikazana izučavanja uticaja mikro- i nano-čestica aluminijum-oksida (Al2O3) na neka svojstva poli(metal-metakrilata) (PMMA) za dentalnu primenu. Površina Al2O3 je tretirana pomoću 3-metakril-oksipropil-trimetokisilana (γ-MPS), a zatim su čestice dodate metal-metakrilatu (MMA), i pomešane sa prahom PMMA. Zapreminski udeli punioca u mikrokompozitima su bili 0,5; 1; 2; 5 i 7 mas.%, dok su u nanokompozitima iznosili 0,13; 0,25; 0,5; 1; 2 i 5 mas.%. Hemijski tretirane čestice Al2O3 punila su analizirane pomoću infracrvene spektroskopije (FTIR). Uticaj veličine i sadržaja punila na mehanička svojstva kompozita je analiziran u ogledima na udar i testovima savijanja. Termička stabilnost PMMA/Al2O3 kompozita je ispitivana pomoću termogravimetrijske analize (TGA). Pored toga, apsorpcija vode i rastvorljivost pripremljenih kompozita je analizirana. Prisustvo novih apsorpcionih traka u FTIR spektrima je potvrdilo uspešnost površinske modifikacije čestica aluminijum-oksida. Obe vrste čestica, mikro- i nano- dimenzija doprinose povećanju otpornosti na udar. Maksimalna vrednost od 2,02 MPa m1/2 je ostvarena dodatkom 0,5 mas.% nano-Al2O3, što odgovara povećanju od 39%. Za razliku od čvrstoće na savijanje, modula savijanja se povećava sa povećanjem sadržaja punioca. Mikrokompoziti su pokazivali veću termičku stabilnost u odnosu na nanokompozite. Apsorpcija vode i rastvorljivost pripremljenih kompozita su bile malo viće u odnosu na kontrolni uzorak PMMA. Dodatak Al2O3 nanočestica u malim količinama može poslužiti za poboljšanje mehaničkih svojstava PMMA pri izradi zubnih proteza.

Ključne reči: dentalna primena, aluminijum-oksid, površinska modifikacija, apsorpcija vode, ogledi savijanja, udarna žilavost.