Modeling of chlorinated phenols adsorption on polyethylene and polyethylene terephtalate microplastic

LONČARSKI MAJA1, TUBIĆ ALEKSANDRA*,1, KRAGULJ ISAKOVSKI MARIJANA1, JOVIĆ BRANISLAV1, APOSTOLOVIĆ TAMARA1, NIKIĆ JASMINA1,

AGBABA JASMINA1

Supplementary material

Table S1. Physico-chemical properties of the investigated chlorophenols

| Compounds | MW, g mol-1 | log Kowa | Via / cm3 mol-1 10-2 | Swa / mg l-1 | pKaa |
| --- | --- | --- | --- | --- | --- |
| 4-CP | 129 | 2.40 | 1.02 | 27100 | 8.85 |
| 2,4-DCP | 163 | 3.06 | 1.14 | 4500 | 7.90 |
| 2,4,6-TCP | 197 | 3.69 | 1.26 | 800 | 6.40 |
| PCP | 266 | 5.12 | 1.39 | 14 | 4.80 |

MW - molecular weight; Kow, octanol-water partition coefficient; Vi - McGowan volume. aKragulj et al.

Analytical procedure, quality assurance and quality control

Determination of the selected chlorinated phenols in water was performed using gas chromatography with mass spectrometry (Agilent Technologies, 7890A GC System/5975C VL MSD) after derivatization and liquid-liquid extraction with hexane. Blank and control experiments were performed in parallel to the sorption experiments. Blank tests, containing same amounts of background solution and solid particles as the samples, but without the addition of chlorinated phenols, were carried out using conditions similar to those described previously, and no target compound was found. Control tests were carried out in 20 mL of background solution containing a same gradient of CP concentrations as the samples, but without solid particles, in order to evaluate the loss of CP resulting from some additional removal processes, such as volatilization and/or sorption to the wall of glass bottles. Recovery of selected CP after derivatization with acetanhydride and liquid-liquid extraction with hexane ranged from 80-116 with the relative standard deviations (RSD) being below 10 % for all CPs. The method detection limits (MDLs) of the applied analytical methods ranged between 0.11-0.53 μg L-1. The correlation coefcient for the chlorinated phenols calibration curve was higher than 0.99. All the reported concentrations of CP were corrected with the recovery efficiency and internal standard.

a)

b)

c)

Fig.S1  Images of the microplastic particles used in experiments: a) PE, b)  PE_PCPs_1  and c)  PE_PCPs_2

Fig. S2. The points of zero charge of the microplastics investigated: a) PE, b) PE_PCPs_1,

c) PE_PCPs_2 and d) PET

Fig.S3 Kinetic study results of 4-CP, 2,4-DCP, 2,4,6-TCP and PCP on a) PE, b) PE_PCPs_1,

c) PE_PCPs_2 and d) PET during 96 h

Fig. S4. Linear plots of sorption pseudo-second-order kinetic model for 2,4-DCP, 2,4,6-TCP and PCP onto a) PE, b) PE_PCPs_1, c) PE_PCPs_2 and d) PET

Fig S5. Linear plots of sorption modelled with intraparticle diffusion kinetics for 2,4-DCP, 2,4,6-TCP and PCP on a) PE, b) PE_PCPs_1, c) PE_PCPs_2 and d) PET

Table S2. Theoretical and experimental qe values obtained with pseudo-second-order model

| Compounds | Sorbents | k1 (h-1) | R2 | qe (theoretical) | qe (experimental) | SD |
| --- | --- | --- | --- | --- | --- | --- |
| 4-CP | PE | 0.0064 | 0.998 | 142.9 | 141.6 | 0.88 |
|  | PE_PCPs_1 | 0.0120 | 0.994 | 84.50 | 89.85 | 3.76 |
|  | PE_PCPs_2 | 0.0130 | 0.987 | 77.40 | 79.33 | 1.36 |
|  | PET | 0.0140 | 0.998 | 69.69 | 69.71 | 0.01 |
| 2,4-DCP | PE | 0.0045 | 0.999 | 222.2 | 223.2 | 0.66 |
|  | PE_PCPs_1 | 0.0054 | 0.995 | 188.7 | 189.6 | 0.69 |
|  | PE_PCPs_2 | 0.0044 | 0.992 | 223.7 | 226.1 | 1.68 |
|  | PET | 0.0080 | 0.998 | 126.3 | 125.6 | 0.44 |
| 2,4,6-TCP | PE | 0.0066 | 0.991 | 156.3 | 157.7 | 1.03 |
|  | PE_PCPs_1 | 0.0057 | 0.998 | 175.4 | 176.8 | 0.95 |
|  | PE_PCPs_2 | 0.0053 | 0.999 | 199.0 | 207.9 | 6.29 |
|  | PET | 0.0153 | 0.998 | 65.57 | 67.43 | 1.32 |
| PCP | PE | 0.0110 | 0.998 | 90.09 | 90.66 | 0.40 |
|  | PE_PCPs_1 | 0.0130 | 0.995 | 81.30 | 80.66 | 0.45 |
|  | PE_PCPs_2 | 0.0100 | 0.992 | 104.1 | 103.0 | 0.74 |
|  | PET | 0.0430 | 0.990 | 23.94 | 25.75 | 1.28 |

Table S3. Freundlich and Langmuir parameters for adsorption of CPs on MPs

| Compounds | Sorbents | Freundlich model |
| --- | --- | --- |
|  |  | R2 | n | KF / (µg g-1/µg l-1)n | log Kd |
|  |  |  |  |  | 0.01 Sw | 0.05 Sw | 0.5 Sw |
| 4-CP | PE | 0.967 | 0.60 | 4.02 | 1.51 | 1.18 | 0.95 |
|  | PE_PCPs_1 | 0.967 | 0.94 | 1.65 | 1.28 | 1.05 | 0.71 |
|  | PE_PCPs_2 | 0.982 | 0.75 | 3.88 | 1.29 | 1.02 | 0.63 |
|  | PET | 0.999 | 0.90 | 1.29 | 1.86 | 1.69 | 1.45 |
| 2,4-DCP | PE | 0.969 | 0.63 | 0.94 | 1.63 | 1.35 | 1.16 |
|  | PE_PCPs_1 | 0.985 | 0.58 | 3.45 | 1.59 | 1.30 | 0.86 |
|  | PE_PCPs_2 | 0.977 | 0.75 | 1.02 | 1.29 | 1.12 | 0.86 |
|  | PET | 0.971 | 0.92 | 0.29 | 2.10 | 2.05 | 1.96 |
| 2,4,6-TCP | PE | 0.947 | 0.66 | 1.39 | 1.82 | 1.58 | 1.24 |
|  | PE_PCPs_1 | 0.961 | 0.6 | 1.69 | 1.67 | 1.40 | 0.99 |
|  | PE_PCPs_2 | 0.99 | 0.6 | 1.50 | 1.61 | 1.32 | 0.92 |
|  | PET | 0.989 | 0.85 | 0.99 | 2.41 | 2.31 | 2.16 |
| PCP | PE | 0.959 | 0.57 | 1.78 | 2.34 | 2.04 | 1.61 |
|  | PE_PCPs_1 | 0.931 | 0.53 | 1.57 | 2.18 | 1.85 | 1.38 |
|  | PE_PCPs_2 | 0.945 | 0.54 | 0.63 | 1.81 | 1.49 | 1.02 |
|  | PET | 0.953 | 0.94 | 0.93 | 2.84 | 2.79 | 2.73 |
| Compounds | Sorbents | Langmuir model |
|  |  | R2 | qmax / µg g-1 | KL / l µg-1 | RL |
| 4-CP | PE | 0.997 | 63.30 | 0.0530 | 0.203-0.972 |
|  | PE_PCPs_1 | 0.974 | 282.9 | 0.0059 | 0.210-0.965 |
|  | PE_PCPs_2 | 0.967 | 86.90 | 0.0058 | 0.745-0.997 |
|  | PET | 0.999 | 335.5 | 0.0030 | 0.828-0.998 |
| 2,4-DCP | PE | 0.921 | 44.90 | 0.0066 | 0.624-0.996 |
|  | PE_PCPs_1 | 0.992 | 55.30 | 0.0339 | 0.267-0.986 |
|  | PE_PCPs_2 | 0.967 | 86.90 | 0.0058 | 0.668-0.996 |
|  | PET | 0.973 | 104.7 | 0.0023 | 0.826-0.998 |
| 2,4,6-TCP | PE | 0.984 | 22.90 | 0.0391 | 0.223-0.974 |
|  | PE_PCPs_1 | 0.974 | 38.70 | 0.0186 | 0.377-0.989 |
|  | PE_PCPs_2 | 0.993 | 27.80 | 0.0294 | 0.276-0.984 |
|  | PET | 0.990 | 198.4 | 0.0039 | 0.763-0.998 |
| PCP | PE | 0.949 | 15.60 | 0.1354 | 0.077-0.937 |
|  | PE_PCPs_1 | 0.948 | 23.70 | 0.0243 | 0.306-0.985 |
|  | PE_PCPs_2 | 0.939 | 7.70 | 0.0691 | 0.130-0.951 |
|  | PET | 0.956 | 309.9 | 0.0027 | 0.825-0.999 |