1) The title must be corrected to describe what type of study is investigated (structure, electrochemical properties, etc.)

Due to the word limit in the title, we cannot expand it without breaking the journal rules.

2) The synthesis process should contain all steps during the synthesis

We have added some aspects of the synthesis to the text. The synthesis is described in more detail in our article5 (V. Galaguz, S. Malovanyi, E. Panov, Synthesis of LiFePO4 nanocrystals and properties of cathodic material on their basis, J. Serb. Chem. Soc., 83 (2018), 1123).

3) For sample 1, XRD and Raman spectrum are necessary to show.

Material synthesis and XRD spectrum for synthesized LiFePO4 are presented in article5 in detail; we did not repeat this information here. We used Raman spectroscopy to investigate the carbon coating. Therefore, the spectra for sample 1 without carbon were not taken.

4) All peaks in the XPS spectrum must be explained.

There are explanations for all spectra in the tables and the text of the manuscript. The interpretation is ambiguous only for components with energies Eb Fe2p3/2 706.7 and 708.2 eV, which is also described in the text.

5) The abstract and the conclusion must be clearer.

The text of these chapters was slightly modified and now it is presented here in a clear way.