SUPPLEMENTARY MATERIAL TO

Synthesis, x-ray structure and DFT calculation of magnetic properties of binuclear Ni(II) complex with tridentate hydrazone-based ligand

Tanja Keškić, Dušanka Radanović1, Andrej Pevec2, Iztok Turel2, Maja Gruden, Katarina Anđelković, Dragana Mitić3, Matija Zlatar1* and Božidar Čobeljić

Faculty of Chemistry, University of Belgrade, Studentski trg 12-16, 11000 Belgrade, Serbia

1Institute of Chemistry, Technology and Metallurgy, University of Belgrade, Njegoševa 12,  11000 Belgrade, Serbia

2Faculty of Chemistry and Chemical Technology, University of Ljubljana, Večna pot 113, 1000 Ljubljana, Slovenia

3Innovation center of the Faculty of Chemistry, University of Belgrade, Studentski trg 12-16, 11000 Belgrade, Serbia

CONTENTS

Isolated yields and spectroscopic data of synthesized compounds

Supporting information for X-ray crystallography

ISOLATED YIELDS AND SPECTROSCOPIC DATA OF SYNTHESIZED COMPOUNDS

(E)-N,N,N-trimethyl-2-oxo-2-(2-(1-(pyridin-2-yl)ethylidene)hydrazinyl)ethan-1-aminium-chloride (HLCl). Yield 1.17 g (87%). White solid. IR (ATR, cm–1): 3387w, 3127m, 3090m, 3049m, 3016m, 2950s, 1700vs, 1612w, 1549s, 1485m, 1400m, 1300w, 1253w, 1200s, 1153w, 1135m, 1095w, 1073m, 975w, 944w, 914m, 748w, 683w. Anal. Calcd. for C12H19ClN4O (FW: 270.76): C, 53.23; H, 7.07; N, 20.69 %. Found: C, 53.34; H, 7.38; N, 20.49 %. 1H NMR: 11.41 (N-H, s), 4.92 (C10-H2, s), 3.35 (C11-H9, s), 2.37 (C8-H3, s), 8.62 (C3-H, m), 7.45 (C4-H, m), 7.91 (C5-H, td, J3 = 10 Hz, J4 = 5 Hz), 8.12 (C6-H, d, J3 = 10 Hz). 13C NMR: 63.2 (C10), 53.7 (C11), 13.9 (C8), 149.2 (C3), 124.9 (C4), 137.2 (C5), 120.8 (C6), 154.9 (C7), 155.3 (C2), 167.1 (C9).

[Ni2L2(μ-1,1-N3)2(N3)2](6H2O complex (1). Yield 126 mg (73 %). IR (ATR, cm–1): 3344s, 3036w, 2039vs, 1619w, 1595w, 1540s, 1469m, 1441m, 1399w, 1335w, 1300m, 1247w, 1200w, 1145w, 1074w, 1026w, 973w, 909w, 781w, 750w, 676w, 571w. Anal. Calcd. for C24H48N20Ni2O8 (FW: 862.24): C, 33.43; H, 5.61; N 32.49 %. Found: C, 33.31; H, 5.69; N 32.24.

SUPPORTING INFORMATION FOR X-RAY CRYSTALOGRAPHY

TABLE S1. Crystal data and structure refinement details for 1.

|  | 1 |
| --- | --- |
| formula | C24H48N20Ni2O8 |
| Fw (g mol–1) | 862.24 |
| crystal size (mm) | 0.20 ( 0.20 ( 0.05 |
| crystal color | yellow |
| crystal system | triclinic |
| space group | P –1 |
| a (Å) | 8.9538(7) |
| b (Å) | 9.0014(6) |
| c (Å) | 13.1769(11) |
| α (º) | 76.170(6) |
| β (º) | 73.159(7) |
| γ (º) | 82.598(6) |
| V (Å3) | 984.97(14) |
| Z | 1 |
| calcd density (g cm-3) | 1.454 |
| F(000) | 452 |
| no. of collected reflns | 9259 |
| no. of independent reflns | 5142 |
| Rint | 0.0420 |
| no. of reflns observed | 4217 |
| no. parameters | 266 |
| R[I > 2σ (I)]a | 0.0495 |
| wR2 (all data)b | 0.1314 |
| Goof , Sc | 1.039 |
| maximum/minimum residual electron density (e Å–3) | +1.65/–0.65 |

a R = ∑||Fo| – |Fc||/∑|Fo|. b wR2 = {∑[w(Fo2 – Fc2)2]/∑[w(Fo2)2]}1/2.

c S = {∑[w(Fo2 – Fc2)2]/(n/p)}1/2 where n is the number of reflections and p is the total number of parameters refined.

TABLE S2. Hydrogen-bond parameters for complex 1.

| D–H(((A | D–H (Å) | H(((A (Å) | D(((A (Å) | D–H(((A (() | Symm. operation on A |
| --- | --- | --- | --- | --- | --- |
| O1W–H1W(((N3 | 0.86(5) | 2.13(5) | 2.982(4) | 171(4) |  |
| O2W–H3W(((N5 | 0.84(4) | 2.04(4) | 2.885(4) | 177(5) |  |
| O2W–H4W(((O3W | 0.84(5) | 1.97(5) | 2.726(5) | 150(5) |  |
| O3W–H5W(((N7 | 0.85(4) | 2.18(4) | 2.992(5) | 160(5) | x, 1+y, z |
| O3W–H6W(((O1W | 0.86(4) | 1.96(4) | 2.748(5) | 153(6) | 1+x, y, z |
| Intra C1–H1(((O1 | 0.95 | 2.55 | 3.288(3) | 135 | 1-x, -y, 1-z |
| C2–H2(((N10 | 0.95 | 2.57 | 3.451(5) | 155 | 2-x,-y,1-z |
| C11(((H11A(((N10 | 0.98 | 2.61 | 3.517(5) | 154 | -1+x, y, z |
| Intra C11–H11B(((O1 | 0.98 | 2.39 | 2.989(4) | 119 |  |
| C12–H12C(((N7 | 0.98 | 2.52 | 3.429(4) | 154 | 1-x,-y,-z |

a)

b)

c)

Fig S1. Crystal packing of 1 showing a) 2D layer parallel with the (001) lattice plain generated by intermolecular hydrogen bonding. b) Side view of the layers parallel with the (001) lattice plane showing channels propagating parallel with a axis filled with solvent water molecules. Hydrogen atoms have been omitted for the sake of clarity, except those involved in hydrogen bonding. c) C7–H7B(((((py) intermolecular contact connecting dimers of 1 along [010] direction.

# Footnotes

Corresponding authorс. E-mail: matijaz@chem.bg.ac.rs and bozidar@chem.bg.ac.rs